DATA SHEET

SHIN-ETSU SILICONE

RTV RUBBER COMPOUND

KE45T

Codes:		CCL/KE45T/10T	-	100g Tube

CCL/KE45T/33C	-	330ml Cartridge

Shin-Etsu KE45T Silicone Rubber Compound is an electronics

Grade oxime cure RTV material, which is used extensively throughout

the electronics industry in Japan and now here within the UK. Notably

with most Japanese UK Based electronic manufacturers.

KE45T provides a fast cure, non-corrosive sealing and adhesive compound

Essential for applications where a high quality reliable sealant is demanded.

Typical Specifications

*	Appearance						:		Paste

*	Cure System						:		Oxime

*	Specific Gravity					:		1.05

*	Hardness 			(JIS-A)		:		30.00

*	Tensile Strength 		(kgf/cm2)		:		20.00

*	Elongation			(%)			:		400.00

*	Volume Resistivity 		(ohms-cm)		:		5 x 1014

*	Dielectric Strength 		(KV/mm)		:		23.00

*	Dielectric Constant 		(1 MHz)		:		3.0

*	Dissipation Factor 		(1MHz)		:		5 x 10-3

*	Thermal Conductivity 	(cal/cm.sec.°C)	:		5 x 10-4

*	Tack Free Time 		(mins)			:		7.00

*	Shear Adhesive Strength 	(kgf/cm2)		:		10.00

- Sizes : 100gm tube, 330ml Cartridge

All information given in good faith but without warranty